**Appendix**

Table A1 Raw input and output data obtained from published literatures.

| Input | | | | | | | | | | | | Output | |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. | Type of fiber | Fiber diameter (µm) | Embedded length (µm) | Young’s modulus of fiber (GPa) | Poisson’s ratio of fiber | Type of matrix | Young’s modulus of matrix (GPa) | Poisson’s ratio of matrix | Loading rate (m/s) | Prepare temperature (℃) | Test temperature (℃) | Fmax (N) | IFSS (MPa) |
| 1 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 3 | 0.34 | 6 | 370 | 30 | 0.054 | 67.1 |
| 2 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 3 | 0.34 | 6 | 370 | 30 | 0.049 | 60.8 |
| 3 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2.5 | 0.34 | 6 | 370 | 50 | 0.055 | 68.6 |
| 4 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2.3 | 0.34 | 6 | 370 | 70 | 0.058 | 71.8 |
| 5 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2.3 | 0.34 | 6 | 370 | 70 | 0.048 | 60.2 |
| 6 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2.3 | 0.34 | 6 | 370 | 70 | 0.045 | 56.5 |
| 7 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2.3 | 0.34 | 6 | 370 | 70 | 0.043 | 53.6 |
| 8 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2 | 0.34 | 6 | 370 | 100 | 0.069 | 86.2 |
| 9 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2 | 0.34 | 6 | 370 | 100 | 0.067 | 83.3 |
| 10 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2 | 0.34 | 6 | 370 | 100 | 0.057 | 70.9 |
| 11 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2 | 0.34 | 6 | 370 | 100 | 0.051 | 63.8 |
| 12 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2 | 0.34 | 6 | 370 | 100 | 0.048 | 59.7 |
| 13 | 1 | 6 | 42.5 | 294 | 0.3 | 1 | 2 | 0.34 | 6 | 370 | 100 | 0.039 | 48.9 |
| 14 | 2 | 7 | 50.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.065 | 58.8 |
| 15 | 2 | 7 | 51.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.071 | 63.1 |
| 16 | 2 | 7 | 51.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.073 | 64.0 |
| 17 | 2 | 7 | 51.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.069 | 60.6 |
| 18 | 2 | 7 | 52.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.077 | 66.9 |
| 19 | 2 | 7 | 54.1 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.077 | 65.0 |
| 20 | 2 | 7 | 54.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.079 | 65.8 |
| 21 | 2 | 7 | 54.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.082 | 68.1 |
| 22 | 2 | 7 | 56.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.084 | 67.9 |
| 23 | 2 | 7 | 56.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.083 | 64.0 |
| 24 | 2 | 7 | 56.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.079 | 66.9 |
| 25 | 2 | 7 | 57.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.076 | 60.2 |
| 26 | 2 | 7 | 57.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.083 | 65.2 |
| 27 | 2 | 7 | 58.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.078 | 60.2 |
| 28 | 2 | 7 | 59.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.081 | 61.9 |
| 29 | 2 | 7 | 59.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.086 | 64.8 |
| 30 | 2 | 7 | 60.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.081 | 61.2 |
| 31 | 2 | 7 | 61.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.089 | 66.0 |
| 32 | 2 | 7 | 62.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.083 | 69.0 |
| 33 | 2 | 7 | 62.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.094 | 60.0 |
| 34 | 2 | 7 | 63.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.087 | 63.1 |
| 35 | 2 | 7 | 63.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.087 | 61.9 |
| 36 | 2 | 7 | 64.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.098 | 69.8 |
| 37 | 2 | 7 | 64.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.092 | 65.0 |
| 38 | 2 | 7 | 64.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.089 | 63.1 |
| 39 | 2 | 7 | 65.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.089 | 61.9 |
| 40 | 2 | 7 | 66.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.092 | 62.9 |
| 41 | 2 | 7 | 67.7 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.091 | 67.9 |
| 42 | 2 | 7 | 67.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.094 | 66.0 |
| 43 | 2 | 7 | 67.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.101 | 70.0 |
| 44 | 2 | 7 | 67.7 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.104 | 63.1 |
| 45 | 2 | 7 | 68.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.093 | 62.3 |
| 46 | 2 | 7 | 68.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.105 | 70.0 |
| 47 | 2 | 7 | 69.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.090 | 63.1 |
| 48 | 2 | 7 | 70.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.093 | 60.6 |
| 49 | 2 | 7 | 70.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.098 | 63.1 |
| 50 | 2 | 7 | 71.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.092 | 62.9 |
| 51 | 2 | 7 | 72.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.111 | 69.8 |
| 52 | 2 | 7 | 73.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.100 | 61.9 |
| 53 | 2 | 7 | 74.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.110 | 66.9 |
| 54 | 2 | 7 | 75.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.103 | 62.9 |
| 55 | 2 | 7 | 75.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.097 | 58.8 |
| 56 | 2 | 7 | 76.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.100 | 60.4 |
| 57 | 2 | 7 | 76.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.104 | 61.7 |
| 58 | 2 | 7 | 77.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.100 | 66.0 |
| 59 | 2 | 7 | 77.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.123 | 70.0 |
| 60 | 2 | 7 | 78.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.114 | 66.0 |
| 61 | 2 | 7 | 79.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.108 | 61.9 |
| 62 | 2 | 7 | 79.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.108 | 61.5 |
| 63 | 2 | 7 | 79.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.115 | 63.8 |
| 64 | 2 | 7 | 80.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | 25 | 0.106 | 66.0 |
| 65 | 2 | 7 | 50.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.077 | 76.6 |
| 66 | 2 | 7 | 50.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.082 | 81.7 |
| 67 | 2 | 7 | 51.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.084 | 84.5 |
| 68 | 2 | 7 | 51.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.076 | 76.2 |
| 69 | 2 | 7 | 52.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.088 | 88.3 |
| 70 | 2 | 7 | 53.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.097 | 96.6 |
| 71 | 2 | 7 | 54.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.091 | 90.9 |
| 72 | 2 | 7 | 55.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.099 | 98.6 |
| 73 | 2 | 7 | 56.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.092 | 92.0 |
| 74 | 2 | 7 | 56.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.101 | 100.6 |
| 75 | 2 | 7 | 56.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.094 | 93.8 |
| 76 | 2 | 7 | 57.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.089 | 88.9 |
| 77 | 2 | 7 | 57.7 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.096 | 95.7 |
| 78 | 2 | 7 | 58.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.091 | 90.5 |
| 79 | 2 | 7 | 59.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.095 | 95.3 |
| 80 | 2 | 7 | 60.1 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.099 | 99.3 |
| 81 | 2 | 7 | 60.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.095 | 95.3 |
| 82 | 2 | 7 | 61.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.103 | 103.0 |
| 83 | 2 | 7 | 62.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.109 | 108.5 |
| 84 | 2 | 7 | 62.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.096 | 96.2 |
| 85 | 2 | 7 | 63.1 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.102 | 101.7 |
| 86 | 2 | 7 | 63.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.101 | 100.8 |
| 87 | 2 | 7 | 64.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.114 | 113.6 |
| 88 | 2 | 7 | 64.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.108 | 108.0 |
| 89 | 2 | 7 | 64.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.105 | 104.7 |
| 90 | 2 | 7 | 65.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.104 | 104.1 |
| 91 | 2 | 7 | 66.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.107 | 107.4 |
| 92 | 2 | 7 | 67.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.109 | 108.7 |
| 93 | 2 | 7 | 67.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.116 | 116.4 |
| 94 | 2 | 7 | 67.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.120 | 119.9 |
| 95 | 2 | 7 | 68.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.115 | 115.1 |
| 96 | 2 | 7 | 68.1 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.103 | 103.4 |
| 97 | 2 | 7 | 68.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.119 | 118.8 |
| 98 | 2 | 7 | 68.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.111 | 110.5 |
| 99 | 2 | 7 | 70.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.119 | 119.1 |
| 100 | 2 | 7 | 70.9 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.114 | 114.2 |
| 101 | 2 | 7 | 71.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.115 | 114.7 |
| 102 | 2 | 7 | 72.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.127 | 127.4 |
| 103 | 2 | 7 | 73.5 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.117 | 116.8 |
| 104 | 2 | 7 | 74.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.126 | 126.3 |
| 105 | 2 | 7 | 74.7 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.121 | 120.6 |
| 106 | 2 | 7 | 75.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.115 | 114.6 |
| 107 | 2 | 7 | 75.4 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.111 | 110.9 |
| 108 | 2 | 7 | 76.2 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.124 | 123.9 |
| 109 | 2 | 7 | 77.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.130 | 130.1 |
| 110 | 2 | 7 | 77.8 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.137 | 137.5 |
| 111 | 2 | 7 | 78.1 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.131 | 131.1 |
| 112 | 2 | 7 | 79.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.122 | 121.7 |
| 113 | 2 | 7 | 79.0 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.126 | 125.6 |
| 114 | 2 | 7 | 79.3 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.130 | 129.8 |
| 115 | 2 | 7 | 79.6 | 230 | 0.2 | 2 | 2.74 | 0.35 | 0.014 | 230 | -196 | 0.134 | 133.6 |
| 116 | 3 | 7 | 43.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.025 | 25.8 |
| 117 | 3 | 7 | 56.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.042 | 33.7 |
| 118 | 3 | 7 | 59.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.037 | 28.3 |
| 119 | 3 | 7 | 60.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.052 | 39.2 |
| 120 | 3 | 7 | 61.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.045 | 32.9 |
| 121 | 3 | 7 | 63.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.037 | 26.7 |
| 122 | 3 | 7 | 65.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.048 | 33.3 |
| 123 | 3 | 7 | 66.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.047 | 32.1 |
| 124 | 3 | 7 | 68.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.051 | 34.2 |
| 125 | 3 | 7 | 69.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.055 | 36.5 |
| 126 | 3 | 7 | 69.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.058 | 38.0 |
| 127 | 3 | 7 | 69.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.056 | 36.8 |
| 128 | 3 | 7 | 71.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.064 | 40.7 |
| 129 | 3 | 7 | 71.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.061 | 38.6 |
| 130 | 3 | 7 | 73.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.050 | 30.8 |
| 131 | 3 | 7 | 74.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.058 | 35.3 |
| 132 | 3 | 7 | 74.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.062 | 37.9 |
| 133 | 3 | 7 | 74.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.061 | 37.1 |
| 134 | 3 | 7 | 74.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.059 | 35.8 |
| 135 | 3 | 7 | 74.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.055 | 33.8 |
| 136 | 3 | 7 | 74.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.051 | 31.1 |
| 137 | 3 | 7 | 75.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.048 | 29.1 |
| 138 | 3 | 7 | 73.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.068 | 42.1 |
| 139 | 3 | 7 | 79.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.066 | 38.1 |
| 140 | 3 | 7 | 80.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.070 | 39.5 |
| 141 | 3 | 7 | 82.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.080 | 44.3 |
| 142 | 3 | 7 | 83.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.081 | 43.7 |
| 143 | 3 | 7 | 83.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 310 | 25 | 0.065 | 35.5 |
| 144 | 3 | 7 | 42.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.039 | 41.5 |
| 145 | 3 | 7 | 45.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.042 | 41.7 |
| 146 | 3 | 7 | 44.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.041 | 42.0 |
| 147 | 3 | 7 | 45.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.041 | 40.6 |
| 148 | 3 | 7 | 49.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.046 | 42.9 |
| 149 | 3 | 7 | 52.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.050 | 43.4 |
| 150 | 3 | 7 | 53.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.060 | 51.2 |
| 151 | 3 | 7 | 53.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.060 | 50.9 |
| 152 | 3 | 7 | 53.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.057 | 47.9 |
| 153 | 3 | 7 | 54.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.056 | 46.3 |
| 154 | 3 | 7 | 56.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.060 | 47.7 |
| 155 | 3 | 7 | 58.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.053 | 41.4 |
| 156 | 3 | 7 | 59.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.060 | 45.6 |
| 157 | 3 | 7 | 59.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.058 | 44.3 |
| 158 | 3 | 7 | 61.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.065 | 48.2 |
| 159 | 3 | 7 | 62.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.070 | 51.1 |
| 160 | 3 | 7 | 63.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.070 | 49.8 |
| 161 | 3 | 7 | 64.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.068 | 48.0 |
| 162 | 3 | 7 | 65.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.069 | 47.6 |
| 163 | 3 | 7 | 64.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.069 | 49.0 |
| 164 | 3 | 7 | 65.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.072 | 50.5 |
| 165 | 3 | 7 | 67.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.067 | 45.1 |
| 166 | 3 | 7 | 69.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.074 | 48.5 |
| 167 | 3 | 7 | 69.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.075 | 49.0 |
| 168 | 3 | 7 | 69.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 80 | 25 | 0.065 | 42.1 |
| 169 | 3 | 7 | 45.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.056 | 55.3 |
| 170 | 3 | 7 | 46.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.045 | 44.4 |
| 171 | 3 | 7 | 51.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.058 | 51.9 |
| 172 | 3 | 7 | 52.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.057 | 49.8 |
| 173 | 3 | 7 | 53.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.062 | 52.6 |
| 174 | 3 | 7 | 54.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.056 | 46.5 |
| 175 | 3 | 7 | 56.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.064 | 51.9 |
| 176 | 3 | 7 | 57.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.064 | 50.1 |
| 177 | 3 | 7 | 62.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.080 | 58.3 |
| 178 | 3 | 7 | 63.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.074 | 53.2 |
| 179 | 3 | 7 | 63.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.079 | 56.7 |
| 180 | 3 | 7 | 63.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.071 | 50.8 |
| 181 | 3 | 7 | 66.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.088 | 60.0 |
| 182 | 3 | 7 | 67.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.070 | 46.8 |
| 183 | 3 | 7 | 68.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.077 | 51.2 |
| 184 | 3 | 7 | 70.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.080 | 51.5 |
| 185 | 3 | 7 | 71.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.091 | 58.1 |
| 186 | 3 | 7 | 72.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.087 | 55.2 |
| 187 | 3 | 7 | 73.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.086 | 52.9 |
| 188 | 3 | 7 | 74.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.089 | 54.3 |
| 189 | 3 | 7 | 74.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.086 | 52.3 |
| 190 | 3 | 7 | 74.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.075 | 46.2 |
| 191 | 3 | 7 | 75.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.079 | 47.9 |
| 192 | 3 | 7 | 77.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.093 | 54.6 |
| 193 | 3 | 7 | 87.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 100 | 25 | 0.106 | 55.3 |
| 194 | 3 | 7 | 33.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.036 | 49.2 |
| 195 | 3 | 7 | 41.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.052 | 58.1 |
| 196 | 3 | 7 | 43.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.046 | 48.8 |
| 197 | 3 | 7 | 45.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.048 | 48.5 |
| 198 | 3 | 7 | 47.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.057 | 54.0 |
| 199 | 3 | 7 | 48.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.056 | 52.4 |
| 200 | 3 | 7 | 51.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.054 | 47.9 |
| 201 | 3 | 7 | 51.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.064 | 56.1 |
| 202 | 3 | 7 | 51.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.066 | 57.9 |
| 203 | 3 | 7 | 53.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.056 | 47.4 |
| 204 | 3 | 7 | 54.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.057 | 47.4 |
| 205 | 3 | 7 | 55.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.065 | 53.5 |
| 206 | 3 | 7 | 56.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.065 | 52.4 |
| 207 | 3 | 7 | 55.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.064 | 53.0 |
| 208 | 3 | 7 | 60.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.071 | 53.2 |
| 209 | 3 | 7 | 63.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.066 | 47.2 |
| 210 | 3 | 7 | 65.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.083 | 57.2 |
| 211 | 3 | 7 | 67.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.086 | 57.4 |
| 212 | 3 | 7 | 67.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.078 | 52.2 |
| 213 | 3 | 7 | 66.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.070 | 47.4 |
| 214 | 3 | 7 | 69.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.074 | 48.3 |
| 215 | 3 | 7 | 69.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.078 | 51.3 |
| 216 | 3 | 7 | 71.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.089 | 56.7 |
| 217 | 3 | 7 | 71.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.075 | 47.3 |
| 218 | 3 | 7 | 73.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.093 | 57.3 |
| 219 | 3 | 7 | 74.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.081 | 49.5 |
| 220 | 3 | 7 | 76.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.093 | 55.4 |
| 221 | 3 | 7 | 76.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.092 | 54.9 |
| 222 | 3 | 7 | 76.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 110 | 25 | 0.091 | 54.1 |
| 223 | 3 | 7 | 39.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.050 | 58.1 |
| 224 | 3 | 7 | 42.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.050 | 54.2 |
| 225 | 3 | 7 | 45.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.054 | 54.6 |
| 226 | 3 | 7 | 45.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.059 | 58.9 |
| 227 | 3 | 7 | 47.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.057 | 54.2 |
| 228 | 3 | 7 | 51.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.067 | 59.9 |
| 229 | 3 | 7 | 52.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.064 | 55.4 |
| 230 | 3 | 7 | 53.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.071 | 60.7 |
| 231 | 3 | 7 | 54.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.066 | 55.3 |
| 232 | 3 | 7 | 57.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.067 | 53.4 |
| 233 | 3 | 7 | 57.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.070 | 55.4 |
| 234 | 3 | 7 | 58.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.071 | 55.5 |
| 235 | 3 | 7 | 58.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.069 | 53.4 |
| 236 | 3 | 7 | 57.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.069 | 54.0 |
| 237 | 3 | 7 | 60.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.077 | 57.9 |
| 238 | 3 | 7 | 61.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.070 | 52.2 |
| 239 | 3 | 7 | 62.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.070 | 50.8 |
| 240 | 3 | 7 | 63.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.078 | 55.9 |
| 241 | 3 | 7 | 63.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.080 | 57.5 |
| 242 | 3 | 7 | 64.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.081 | 56.8 |
| 243 | 3 | 7 | 65.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.080 | 55.6 |
| 244 | 3 | 7 | 65.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.075 | 52.4 |
| 245 | 3 | 7 | 65.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.089 | 62.5 |
| 246 | 3 | 7 | 67.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.086 | 58.5 |
| 247 | 3 | 7 | 67.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.085 | 57.7 |
| 248 | 3 | 7 | 67.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.081 | 55.2 |
| 249 | 3 | 7 | 67.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.083 | 55.6 |
| 250 | 3 | 7 | 67.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.079 | 52.8 |
| 251 | 3 | 7 | 69.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.079 | 52.1 |
| 252 | 3 | 7 | 70.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.079 | 51.0 |
| 253 | 3 | 7 | 71.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.091 | 58.0 |
| 254 | 3 | 7 | 71.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.086 | 54.7 |
| 255 | 3 | 7 | 72.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.089 | 55.9 |
| 256 | 3 | 7 | 72.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.088 | 55.1 |
| 257 | 3 | 7 | 78.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 120 | 25 | 0.107 | 62.3 |
| 258 | 3 | 7 | 51.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.059 | 51.9 |
| 259 | 3 | 7 | 53.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.056 | 47.7 |
| 260 | 3 | 7 | 56.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.057 | 46.5 |
| 261 | 3 | 7 | 53.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.065 | 55.0 |
| 262 | 3 | 7 | 56.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.063 | 50.8 |
| 263 | 3 | 7 | 57.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.064 | 51.0 |
| 264 | 3 | 7 | 57.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.069 | 54.8 |
| 265 | 3 | 7 | 59.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.070 | 53.7 |
| 266 | 3 | 7 | 60.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.064 | 48.3 |
| 267 | 3 | 7 | 61.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.063 | 46.8 |
| 268 | 3 | 7 | 62.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.076 | 55.4 |
| 269 | 3 | 7 | 63.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.078 | 55.9 |
| 270 | 3 | 7 | 66.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.068 | 46.4 |
| 271 | 3 | 7 | 67.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.084 | 57.1 |
| 272 | 3 | 7 | 67.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.074 | 50.0 |
| 273 | 3 | 7 | 68.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.082 | 54.7 |
| 274 | 3 | 7 | 70.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.074 | 47.7 |
| 275 | 3 | 7 | 70.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.086 | 55.4 |
| 276 | 3 | 7 | 72.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.091 | 56.7 |
| 277 | 3 | 7 | 77.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.085 | 49.7 |
| 278 | 3 | 7 | 77.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.090 | 52.5 |
| 279 | 3 | 7 | 96.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 150 | 25 | 0.107 | 50.1 |
| 280 | 3 | 7 | 54.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.065 | 54.4 |
| 281 | 3 | 7 | 56.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.063 | 50.8 |
| 282 | 3 | 7 | 57.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.062 | 48.9 |
| 283 | 3 | 7 | 57.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.059 | 46.8 |
| 284 | 3 | 7 | 59.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.062 | 47.2 |
| 285 | 3 | 7 | 59.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.069 | 52.2 |
| 286 | 3 | 7 | 60.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.073 | 54.9 |
| 287 | 3 | 7 | 61.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.075 | 55.8 |
| 288 | 3 | 7 | 62.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.074 | 54.2 |
| 289 | 3 | 7 | 64.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.071 | 50.5 |
| 290 | 3 | 7 | 66.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.072 | 49.4 |
| 291 | 3 | 7 | 66.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.071 | 48.6 |
| 292 | 3 | 7 | 66.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.068 | 46.5 |
| 293 | 3 | 7 | 67.3 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.069 | 46.5 |
| 294 | 3 | 7 | 66.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.076 | 52.0 |
| 295 | 3 | 7 | 67.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.077 | 52.2 |
| 296 | 3 | 7 | 67.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.079 | 53.5 |
| 297 | 3 | 7 | 68.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.074 | 49.0 |
| 298 | 3 | 7 | 68.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.076 | 50.5 |
| 299 | 3 | 7 | 70.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.082 | 52.9 |
| 300 | 3 | 7 | 70.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.084 | 53.9 |
| 301 | 3 | 7 | 82.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.02 | 230 | 25 | 0.093 | 51.7 |
| 302 | 5 | 17.5 | 114.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.130 | 20.6 |
| 303 | 5 | 17.5 | 123.1 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.163 | 24.1 |
| 304 | 5 | 17.5 | 148.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.193 | 23.7 |
| 305 | 5 | 17.5 | 165.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.183 | 20.2 |
| 306 | 5 | 17.5 | 162.2 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.210 | 23.5 |
| 307 | 5 | 17.5 | 179.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.227 | 23.0 |
| 308 | 5 | 17.5 | 184.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.230 | 22.7 |
| 309 | 5 | 17.5 | 193.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.210 | 19.8 |
| 310 | 5 | 17.5 | 198.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.193 | 17.7 |
| 311 | 5 | 17.5 | 198.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.263 | 24.1 |
| 312 | 5 | 17.5 | 215.4 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.257 | 21.7 |
| 313 | 5 | 17.5 | 226.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.240 | 19.3 |
| 314 | 5 | 17.5 | 235.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.223 | 17.3 |
| 315 | 5 | 17.5 | 251.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.237 | 17.1 |
| 316 | 5 | 17.5 | 237.8 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.290 | 22.2 |
| 317 | 5 | 17.5 | 257.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.277 | 19.6 |
| 318 | 5 | 17.5 | 274.1 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.290 | 19.2 |
| 319 | 5 | 17.5 | 254.5 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.303 | 21.7 |
| 320 | 5 | 17.5 | 262.9 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.333 | 23.1 |
| 321 | 5 | 17.5 | 271.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.337 | 22.6 |
| 322 | 5 | 17.5 | 282.5 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.333 | 21.5 |
| 323 | 5 | 17.5 | 285.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.310 | 19.8 |
| 324 | 5 | 17.5 | 293.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.317 | 19.6 |
| 325 | 5 | 17.5 | 299.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.357 | 21.7 |
| 326 | 5 | 17.5 | 313.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.347 | 20.1 |
| 327 | 5 | 17.5 | 321.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.317 | 17.9 |
| 328 | 5 | 17.5 | 330.1 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.303 | 16.7 |
| 329 | 5 | 17.5 | 349.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.333 | 17.3 |
| 330 | 5 | 17.5 | 352.4 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.363 | 18.8 |
| 331 | 5 | 17.5 | 335.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.373 | 20.2 |
| 332 | 5 | 17.5 | 318.9 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.380 | 21.7 |
| 333 | 5 | 17.5 | 332.9 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.383 | 20.9 |
| 334 | 5 | 17.5 | 321.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.390 | 22.1 |
| 335 | 5 | 17.5 | 327.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.403 | 22.4 |
| 336 | 5 | 17.5 | 335.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.410 | 22.2 |
| 337 | 5 | 17.5 | 349.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.420 | 21.8 |
| 338 | 5 | 17.5 | 372.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.473 | 23.1 |
| 339 | 5 | 17.5 | 377.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.453 | 21.8 |
| 340 | 5 | 17.5 | 391.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.443 | 20.6 |
| 341 | 5 | 17.5 | 436.4 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.413 | 17.2 |
| 342 | 5 | 17.5 | 405.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.483 | 21.7 |
| 343 | 5 | 17.5 | 408.4 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.520 | 23.2 |
| 344 | 5 | 17.5 | 556.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.540 | 17.6 |
| 345 | 4 | 7.2 | 65.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.052 | 35.3 |
| 346 | 4 | 7.2 | 65.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.061 | 41.2 |
| 347 | 4 | 7.2 | 63.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.065 | 45.3 |
| 348 | 4 | 7.2 | 81.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.065 | 35.1 |
| 349 | 4 | 7.2 | 81.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.087 | 46.8 |
| 350 | 4 | 7.2 | 91.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.085 | 41.0 |
| 351 | 4 | 7.2 | 93.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.078 | 36.9 |
| 352 | 4 | 7.2 | 106.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.081 | 33.5 |
| 353 | 4 | 7.2 | 120.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.088 | 32.4 |
| 354 | 4 | 7.2 | 115.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.094 | 36.0 |
| 355 | 4 | 7.2 | 111.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.117 | 46.3 |
| 356 | 4 | 7.2 | 120.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.108 | 39.9 |
| 357 | 4 | 7.2 | 128.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.118 | 40.7 |
| 358 | 4 | 7.2 | 158.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.121 | 33.8 |
| 359 | 5 | 17.5 | 155.9 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.179 | 20.9 |
| 360 | 5 | 17.5 | 161.8 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.208 | 23.3 |
| 361 | 5 | 17.5 | 167.8 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.198 | 21.5 |
| 362 | 5 | 17.5 | 233.7 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.344 | 26.8 |
| 363 | 5 | 17.5 | 257.7 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.361 | 25.5 |
| 364 | 5 | 17.5 | 287.6 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.365 | 23.1 |
| 365 | 5 | 17.5 | 259.2 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.389 | 27.3 |
| 366 | 5 | 17.5 | 298.1 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.416 | 25.4 |
| 367 | 5 | 17.5 | 377.5 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.523 | 25.2 |
| 368 | 5 | 17.5 | 182.8 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.208 | 20.7 |
| 369 | 5 | 17.5 | 239.7 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.256 | 19.4 |
| 370 | 5 | 17.5 | 251.7 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.272 | 19.7 |
| 371 | 5 | 17.5 | 262.2 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.279 | 19.4 |
| 372 | 5 | 17.5 | 280.1 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.282 | 18.3 |
| 373 | 5 | 17.5 | 307.1 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.291 | 17.3 |
| 374 | 5 | 17.5 | 349.0 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.361 | 18.8 |
| 375 | 5 | 17.5 | 368.5 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.370 | 18.3 |
| 376 | 5 | 17.5 | 388.0 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.385 | 18.0 |
| 377 | 5 | 17.5 | 456.8 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.440 | 17.5 |
| 378 | 5 | 17.5 | 462.8 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.480 | 18.9 |
| 379 | 5 | 17.5 | 480.8 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.518 | 19.6 |
| 380 | 5 | 17.5 | 212.8 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.198 | 16.9 |
| 381 | 5 | 17.5 | 227.7 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.203 | 16.2 |
| 382 | 5 | 17.5 | 238.2 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.198 | 15.1 |
| 383 | 5 | 17.5 | 263.7 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.234 | 16.1 |
| 384 | 5 | 17.5 | 271.2 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.234 | 15.7 |
| 385 | 5 | 17.5 | 283.1 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.253 | 16.3 |
| 386 | 5 | 17.5 | 286.1 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.272 | 17.3 |
| 387 | 5 | 17.5 | 295.1 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.232 | 14.3 |
| 388 | 5 | 17.5 | 323.6 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.248 | 14.0 |
| 389 | 5 | 17.5 | 347.5 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.294 | 15.4 |
| 390 | 5 | 17.5 | 370.0 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.318 | 15.6 |
| 391 | 5 | 17.5 | 380.5 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.339 | 16.2 |
| 392 | 5 | 17.5 | 404.4 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.344 | 15.5 |
| 393 | 5 | 17.5 | 431.4 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.339 | 14.3 |
| 394 | 5 | 17.5 | 455.3 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.346 | 13.8 |
| 395 | 5 | 17.5 | 194.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.162 | 15.2 |
| 396 | 5 | 17.5 | 209.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.162 | 14.1 |
| 397 | 5 | 17.5 | 253.2 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.179 | 12.9 |
| 398 | 5 | 17.5 | 295.1 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.220 | 13.5 |
| 399 | 5 | 17.5 | 302.6 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.205 | 12.3 |
| 400 | 5 | 17.5 | 310.1 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.203 | 11.9 |
| 401 | 5 | 17.5 | 314.6 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.205 | 11.9 |
| 402 | 5 | 17.5 | 316.1 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.236 | 13.6 |
| 403 | 5 | 17.5 | 326.6 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.203 | 11.3 |
| 404 | 5 | 17.5 | 338.5 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.236 | 12.7 |
| 405 | 5 | 17.5 | 347.5 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.232 | 12.1 |
| 406 | 5 | 17.5 | 356.5 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.265 | 13.5 |
| 407 | 5 | 17.5 | 404.4 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.222 | 10.0 |
| 408 | 5 | 17.5 | 417.9 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.217 | 9.5 |
| 409 | 5 | 17.5 | 425.4 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.291 | 12.5 |
| 410 | 5 | 17.5 | 426.9 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.239 | 10.2 |
| 411 | 5 | 17.5 | 431.4 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.253 | 10.7 |
| 412 | 5 | 17.5 | 453.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.246 | 9.9 |
| 413 | 5 | 17.5 | 456.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.299 | 11.9 |
| 414 | 5 | 17.5 | 459.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.267 | 10.6 |
| 415 | 5 | 17.5 | 462.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.294 | 11.5 |
| 416 | 5 | 17.5 | 470.3 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.265 | 10.3 |
| 417 | 5 | 17.5 | 510.7 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.327 | 11.7 |
| 418 | 5 | 17.5 | 513.7 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.308 | 10.9 |
| 419 | 5 | 17.5 | 170.8 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.129 | 13.7 |
| 420 | 5 | 17.5 | 212.8 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.141 | 12.0 |
| 421 | 5 | 17.5 | 286.1 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.148 | 9.4 |
| 422 | 5 | 17.5 | 304.1 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.148 | 8.9 |
| 423 | 5 | 17.5 | 305.6 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.138 | 8.2 |
| 424 | 5 | 17.5 | 356.5 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.189 | 9.6 |
| 425 | 5 | 17.5 | 391.0 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.198 | 9.2 |
| 426 | 5 | 17.5 | 405.9 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.181 | 8.1 |
| 427 | 5 | 17.5 | 449.3 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.179 | 7.2 |
| 428 | 5 | 17.5 | 465.8 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.215 | 8.4 |
| 429 | 5 | 17.5 | 480.8 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.181 | 6.9 |
| 430 | 5 | 17.5 | 512.2 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.189 | 6.7 |
| 431 | 5 | 17.5 | 533.2 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.234 | 8.0 |
| 432 | 5 | 17.5 | 537.7 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.198 | 6.7 |
| 433 | 5 | 17.5 | 587.1 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.244 | 7.5 |
| 434 | 5 | 17.5 | 124.4 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.081 | 11.9 |
| 435 | 5 | 17.5 | 139.4 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.081 | 10.6 |
| 436 | 5 | 17.5 | 157.4 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.100 | 11.6 |
| 437 | 5 | 17.5 | 197.8 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.098 | 9.0 |
| 438 | 5 | 17.5 | 340.0 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.141 | 7.5 |
| 439 | 5 | 17.5 | 370.0 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.110 | 5.4 |
| 440 | 5 | 17.5 | 402.9 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.091 | 4.1 |
| 441 | 5 | 17.5 | 423.9 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.138 | 5.9 |
| 442 | 5 | 17.5 | 438.9 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.110 | 4.5 |
| 443 | 6 | 5 | 24.5 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.025 | 64.5 |
| 444 | 6 | 5 | 27.9 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.033 | 74.7 |
| 445 | 6 | 5 | 29.9 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.044 | 94.4 |
| 446 | 6 | 5 | 33.2 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.041 | 78.1 |
| 447 | 6 | 5 | 35.1 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.047 | 85.8 |
| 448 | 6 | 5 | 35.1 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.052 | 95.1 |
| 449 | 6 | 5 | 35.2 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.060 | 108.7 |
| 450 | 6 | 5 | 36.0 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.049 | 87.5 |
| 451 | 6 | 5 | 37.0 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.055 | 94.8 |
| 452 | 6 | 5 | 37.4 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.049 | 82.7 |
| 453 | 6 | 5 | 40.1 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.064 | 101.6 |
| 454 | 6 | 5 | 43.4 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.066 | 97.4 |
| 455 | 6 | 5 | 44.2 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.073 | 105.1 |
| 456 | 6 | 5 | 44.7 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.072 | 102.4 |
| 457 | 6 | 5 | 45.8 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.066 | 91.9 |
| 458 | 6 | 5 | 45.7 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.076 | 105.7 |
| 459 | 6 | 5 | 68.8 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.093 | 86.4 |
| 460 | 6 | 5 | 69.8 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.098 | 89.4 |
| 461 | 6 | 5 | 71.3 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.115 | 103.0 |
| 462 | 6 | 5 | 73.0 | 294 | 0.2 | 5 | 3.5 | 0.31 | 0.0017 | 105 | 25 | 0.123 | 107.2 |
| 463 | 7 | 7.5 | 52.3 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.034 | 27.9 |
| 464 | 7 | 7.5 | 54.0 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.066 | 51.7 |
| 465 | 7 | 7.5 | 55.7 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.038 | 29.0 |
| 466 | 7 | 7.5 | 56.8 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.034 | 25.7 |
| 467 | 7 | 7.5 | 58.5 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.032 | 23.1 |
| 468 | 7 | 7.5 | 59.6 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.035 | 25.0 |
| 469 | 7 | 7.5 | 64.2 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.037 | 24.7 |
| 470 | 7 | 7.5 | 65.3 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.034 | 22.1 |
| 471 | 7 | 7.5 | 68.1 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.043 | 26.6 |
| 472 | 7 | 7.5 | 68.1 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.059 | 37.1 |
| 473 | 7 | 7.5 | 69.8 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.068 | 41.2 |
| 474 | 7 | 7.5 | 74.1 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.052 | 29.8 |
| 475 | 7 | 7.5 | 76.9 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.062 | 34.2 |
| 476 | 7 | 7.5 | 80.0 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.084 | 44.4 |
| 477 | 7 | 7.5 | 85.7 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.074 | 36.5 |
| 478 | 7 | 7.5 | 85.7 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.077 | 38.0 |
| 479 | 7 | 7.5 | 97.0 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.095 | 41.8 |
| 480 | 7 | 7.5 | 102.6 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.104 | 43.1 |
| 481 | 7 | 7.5 | 142.8 | 230 | 0.3 | 6 | 3.86 | 0.31 | 0.0017 | 120 | 25 | 0.152 | 45.1 |
| 482 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 3.96 | 0.37 | 0.0333 | 135 | 25 | 0.069 | 39.3 |
| 483 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 3.068 | 0.37 | 0.0333 | 135 | 60 | 0.052 | 29.3 |
| 484 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 2.51 | 0.37 | 0.0333 | 135 | 90 | 0.054 | 30.5 |
| 485 |  | 7 | 80.0 | 233 | 0.2 | 7 | 1.59 | 0.37 | 0.0333 | 135 | 120 | 0.021 | 12.2 |
| 486 |  | 10 | 561.0 | 70 | 0.22 | 8 | 3.2 | 0.35 | 0.08 | 27 | 25 | 0.159 | 9.0 |
| 487 |  | 10 | 731.0 | 70 | 0.22 | 8 | 3.2 | 0.35 | 0.08 | 27 | 25 | 0.241 | 10.5 |
| 488 |  | 10 | 687.0 | 70 | 0.22 | 8 | 3.2 | 0.35 | 0.08 | 27 | 25 | 0.216 | 10.0 |
| 489 | 8 | 10 | 786.0 | 70 | 0.22 | 8 | 3.2 | 0.35 | 0.08 | 27 | 25 | 0.272 | 11.0 |
| 490 | 9 | 10 | 524.0 | 70 | 0.22 | 8 | 3.2 | 0.35 | 0.08 | 27 | 25 | 0.181 | 11.0 |
| 491 | 9 | 12 | 127.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 9.4 |
| 492 | 9 | 12 | 127.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 7.5 |
| 493 | 9 | 12 | 129.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 9.0 |
| 494 | 9 | 12 | 129.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.5 |
| 495 | 10 | 12 | 131.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.0 |
| 496 | 10 | 12 | 135.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.5 |
| 497 | 10 | 12 | 136.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 9.2 |
| 498 | 10 | 12 | 138.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 9.7 |
| 499 | 10 | 12 | 139.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.0 |
| 500 | 10 | 12 | 142.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.0 |
| 501 | 10 | 12 | 143.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.8 |
| 502 | 10 | 12 | 145.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.005 | 8.8 |
| 503 | 10 | 12 | 146.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 9.0 |
| 504 | 10 | 12 | 146.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 7.5 |
| 505 | 10 | 12 | 149.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 7.3 |
| 506 | 10 | 12 | 152.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.3 |
| 507 | 10 | 12 | 152.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.5 |
| 508 | 10 | 12 | 154.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.5 |
| 509 | 10 | 12 | 157.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 7.9 |
| 510 | 10 | 12 | 159.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 9.3 |
| 511 | 10 | 12 | 160.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.0 |
| 512 | 10 | 12 | 162.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 7.7 |
| 513 | 10 | 12 | 164.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 7.3 |
| 514 | 10 | 12 | 167.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.8 |
| 515 | 10 | 12 | 170.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.8 |
| 516 | 10 | 12 | 170.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.6 |
| 517 | 10 | 12 | 171.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.006 | 8.0 |
| 518 | 10 | 12 | 174.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.8 |
| 519 | 10 | 12 | 173.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 9.4 |
| 520 | 10 | 12 | 175.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.1 |
| 521 | 10 | 12 | 177.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 7.7 |
| 522 | 10 | 12 | 178.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.5 |
| 523 | 10 | 12 | 180.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 9.4 |
| 524 | 10 | 12 | 182.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.0 |
| 525 | 10 | 12 | 183.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 7.7 |
| 526 | 10 | 12 | 184.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.2 |
| 527 | 10 | 12 | 189.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.0 |
| 528 | 10 | 12 | 190.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 7.6 |
| 529 | 10 | 12 | 192.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.7 |
| 530 | 10 | 12 | 194.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 7.6 |
| 531 | 10 | 12 | 195.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.007 | 8.5 |
| 532 | 10 | 12 | 201.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.008 | 7.8 |
| 533 | 10 | 12 | 204.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.008 | 8.1 |
| 534 | 10 | 12 | 206.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.008 | 8.5 |
| 535 | 10 | 12 | 209.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.008 | 8.0 |
| 536 | 10 | 12 | 211.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.008 | 7.8 |
| 537 | 10 | 12 | 217.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.008 | 7.7 |
| 538 | 10 | 160 | 1542.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.775 | 4.5 |
| 539 | 10 | 160 | 1552.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.780 | 4.2 |
| 540 | 10 | 160 | 1556.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.782 | 4.5 |
| 541 | 10 | 160 | 1572.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.791 | 4.0 |
| 542 | 10 | 160 | 1583.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.796 | 4.1 |
| 543 | 10 | 160 | 1593.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.801 | 3.6 |
| 544 | 10 | 160 | 1603.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.806 | 3.6 |
| 545 | 10 | 160 | 1603.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.806 | 4.9 |
| 546 | 10 | 160 | 1603.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.806 | 4.4 |
| 547 | 10 | 160 | 1620.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.814 | 4.3 |
| 548 | 10 | 160 | 1634.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.821 | 4.8 |
| 549 | 10 | 160 | 1645.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.827 | 4.5 |
| 550 | 10 | 160 | 1645.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.827 | 3.8 |
| 551 | 10 | 160 | 1651.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.830 | 4.0 |
| 552 | 10 | 160 | 1656.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.832 | 4.1 |
| 553 | 10 | 160 | 1654.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.831 | 4.3 |
| 554 | 10 | 160 | 1665.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.837 | 4.4 |
| 555 | 10 | 160 | 1671.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.840 | 4.6 |
| 556 | 10 | 160 | 1670.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.840 | 4.1 |
| 557 | 10 | 160 | 1674.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.842 | 3.9 |
| 558 | 10 | 160 | 1682.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.846 | 4.3 |
| 559 | 10 | 160 | 1680.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.845 | 4.2 |
| 560 | 10 | 160 | 1690.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.850 | 4.7 |
| 561 | 10 | 160 | 1691.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.850 | 3.9 |
| 562 | 10 | 160 | 1701.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.855 | 4.0 |
| 563 | 10 | 160 | 1711.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.860 | 4.0 |
| 564 | 10 | 160 | 1710.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.860 | 4.4 |
| 565 | 10 | 160 | 1711.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.860 | 3.4 |
| 566 | 10 | 160 | 1721.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.865 | 3.8 |
| 567 | 10 | 160 | 1749.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.880 | 3.6 |
| 568 | 10 | 160 | 1748.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.879 | 3.8 |
| 569 | 10 | 160 | 1744.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.877 | 3.7 |
| 570 | 10 | 160 | 1749.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.879 | 4.1 |
| 571 | 10 | 160 | 1777.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.893 | 4.0 |
| 572 | 10 | 160 | 1774.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.892 | 4.1 |
| 573 | 10 | 160 | 1779.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.895 | 3.6 |
| 574 | 10 | 160 | 1799.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.905 | 4.2 |
| 575 | 10 | 160 | 1804.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.907 | 4.6 |
| 576 | 10 | 160 | 1810.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.910 | 4.0 |
| 577 | 10 | 160 | 1820.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.915 | 4.1 |
| 578 | 10 | 160 | 1820.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.915 | 3.9 |
| 579 | 10 | 160 | 1833.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.921 | 4.1 |
| 580 | 10 | 160 | 1825.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.918 | 3.5 |
| 581 | 10 | 160 | 1851.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.931 | 4.5 |
| 582 | 10 | 160 | 1853.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.932 | 4.0 |
| 583 | 10 | 160 | 1855.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.932 | 3.7 |
| 584 | 10 | 200 | 1504.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.945 | 3.5 |
| 585 | 10 | 200 | 1513.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.951 | 3.5 |
| 586 | 10 | 200 | 1522.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.957 | 3.2 |
| 587 | 10 | 200 | 1524.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.958 | 3.7 |
| 588 | 10 | 200 | 1545.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.971 | 3.8 |
| 589 | 10 | 200 | 1549.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.973 | 3.5 |
| 590 | 10 | 200 | 1552.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.976 | 3.0 |
| 591 | 10 | 200 | 1560.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.981 | 3.2 |
| 592 | 10 | 200 | 1565.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.984 | 3.6 |
| 593 | 10 | 200 | 1571.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.988 | 3.7 |
| 594 | 10 | 200 | 1571.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.987 | 3.5 |
| 595 | 10 | 200 | 1580.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 0.993 | 3.3 |
| 596 | 10 | 200 | 1602.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.007 | 3.7 |
| 597 | 10 | 200 | 1611.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.013 | 3.9 |
| 598 | 10 | 200 | 1615.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.015 | 3.0 |
| 599 | 10 | 200 | 1621.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.019 | 3.3 |
| 600 | 10 | 200 | 1624.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.021 | 3.1 |
| 601 | 10 | 200 | 1643.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.033 | 3.2 |
| 602 | 10 | 200 | 1643.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.033 | 3.3 |
| 603 | 10 | 200 | 1655.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.040 | 3.2 |
| 604 | 10 | 200 | 1654.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.039 | 3.0 |
| 605 | 10 | 200 | 1667.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.048 | 3.2 |
| 606 | 10 | 200 | 1688.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.061 | 3.4 |
| 607 | 10 | 200 | 1688.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.061 | 3.0 |
| 608 | 10 | 200 | 1691.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.063 | 3.0 |
| 609 | 10 | 200 | 1692.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.064 | 2.8 |
| 610 | 10 | 200 | 1704.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.071 | 3.3 |
| 611 | 10 | 200 | 1703.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.070 | 3.2 |
| 612 | 10 | 200 | 1727.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.086 | 3.1 |
| 613 | 10 | 200 | 1726.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.085 | 3.7 |
| 614 | 10 | 200 | 1733.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.089 | 3.6 |
| 615 | 10 | 200 | 1733.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.089 | 3.4 |
| 616 | 10 | 200 | 1742.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.095 | 3.3 |
| 617 | 10 | 200 | 1746.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.097 | 3.6 |
| 618 | 10 | 200 | 1751.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.100 | 3.3 |
| 619 | 10 | 200 | 1759.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.106 | 3.5 |
| 620 | 10 | 200 | 1764.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.109 | 3.4 |
| 621 | 10 | 200 | 1766.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.110 | 3.1 |
| 622 | 10 | 200 | 1771.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.113 | 3.1 |
| 623 | 10 | 200 | 1775.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.116 | 3.3 |
| 624 | 10 | 200 | 1790.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.125 | 3.3 |
| 625 | 10 | 200 | 1789.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.124 | 2.9 |
| 626 | 10 | 200 | 1795.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.128 | 3.3 |
| 627 | 10 | 200 | 1811.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.138 | 3.3 |
| 628 | 10 | 200 | 1817.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.142 | 3.3 |
| 629 | 10 | 200 | 1809.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.137 | 3.2 |
| 630 | 10 | 200 | 1816.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.142 | 3.0 |
| 631 | 10 | 200 | 1820.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.144 | 3.2 |
| 632 | 10 | 200 | 1827.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.148 | 3.0 |
| 633 | 10 | 300 | 1604.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.512 | 3.0 |
| 634 | 10 | 300 | 1608.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.516 | 3.3 |
| 635 | 10 | 300 | 1617.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.525 | 3.3 |
| 636 | 10 | 300 | 1627.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.533 | 2.9 |
| 637 | 10 | 300 | 1634.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.540 | 3.0 |
| 638 | 10 | 300 | 1634.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.540 | 3.2 |
| 639 | 10 | 300 | 1667.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.572 | 3.0 |
| 640 | 10 | 300 | 1683.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.587 | 3.1 |
| 641 | 10 | 300 | 1709.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.611 | 2.8 |
| 642 | 10 | 300 | 1708.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.610 | 3.1 |
| 643 | 10 | 300 | 1714.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.615 | 3.2 |
| 644 | 10 | 300 | 1726.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.627 | 3.0 |
| 645 | 10 | 300 | 1731.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.632 | 3.0 |
| 646 | 10 | 300 | 1747.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.647 | 2.8 |
| 647 | 10 | 300 | 1757.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.657 | 2.7 |
| 648 | 10 | 300 | 1759.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.658 | 3.2 |
| 649 | 10 | 300 | 1769.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.668 | 3.1 |
| 650 | 10 | 300 | 1778.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.677 | 2.8 |
| 651 | 10 | 300 | 1782.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.679 | 3.3 |
| 652 | 10 | 300 | 1797.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.694 | 3.0 |
| 653 | 10 | 300 | 1805.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.701 | 3.0 |
| 654 | 10 | 300 | 1806.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.702 | 3.4 |
| 655 | 10 | 300 | 1824.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.720 | 3.1 |
| 656 | 10 | 300 | 1826.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.721 | 3.2 |
| 657 | 10 | 300 | 1847.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.742 | 3.2 |
| 658 | 10 | 300 | 1830.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.725 | 2.6 |
| 659 | 10 | 300 | 1834.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.729 | 2.7 |
| 660 | 10 | 300 | 1846.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.741 | 2.4 |
| 661 | 10 | 300 | 1848.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.742 | 2.9 |
| 662 | 10 | 300 | 1856.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.750 | 2.9 |
| 663 | 10 | 300 | 1867.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.760 | 3.1 |
| 664 | 10 | 300 | 1869.1 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.762 | 2.5 |
| 665 | 10 | 300 | 1881.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.773 | 3.0 |
| 666 | 10 | 300 | 1891.3 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.783 | 2.8 |
| 667 | 10 | 300 | 1915.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.805 | 3.3 |
| 668 | 10 | 300 | 1921.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.811 | 2.6 |
| 669 | 10 | 300 | 1922.7 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.812 | 2.9 |
| 670 | 10 | 300 | 1929.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.819 | 2.9 |
| 671 | 10 | 300 | 1930.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.820 | 3.0 |
| 672 | 10 | 300 | 1940.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.828 | 3.3 |
| 673 | 10 | 300 | 1955.2 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.843 | 2.7 |
| 674 | 10 | 300 | 1974.4 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.861 | 2.5 |
| 675 | 10 | 300 | 1979.5 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.866 | 2.3 |
| 676 | 10 | 300 | 1988.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.874 | 2.6 |
| 677 | 10 | 300 | 1990.6 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.876 | 2.9 |
| 678 | 10 | 300 | 2002.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.888 | 3.0 |
| 679 | 10 | 300 | 2003.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.889 | 2.8 |
| 680 | 10 | 300 | 2008.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.893 | 2.9 |
| 681 | 10 | 300 | 2004.8 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.889 | 3.5 |
| 682 | 10 | 300 | 2018.0 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.902 | 3.1 |
| 683 | 10 | 300 | 2011.9 | 3.39 | 0.37 | 9 | 3.29 | 0.31 | 0.0167 | 26 | 25 | 1.896 | 2.3 |
| 684 | 10 | 7.15 | 41.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.006 | 6.4 |
| 685 | 10 | 7.15 | 44.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.006 | 6.0 |
| 686 | 10 | 7.15 | 47.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.009 | 8.6 |
| 687 | 10 | 7.15 | 50.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.009 | 8.0 |
| 688 | 3 | 7.15 | 51.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.010 | 8.6 |
| 689 | 3 | 7.15 | 52.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.010 | 8.4 |
| 690 | 3 | 7.15 | 52.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.012 | 10.1 |
| 691 | 3 | 7.15 | 54.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.009 | 7.3 |
| 692 | 3 | 7.15 | 57.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.014 | 10.8 |
| 693 | 3 | 7.15 | 63.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.011 | 7.6 |
| 694 | 3 | 7.15 | 69.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.014 | 8.9 |
| 695 | 3 | 7.15 | 71.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.013 | 8.1 |
| 696 | 3 | 7.15 | 72.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.010 | 6.1 |
| 697 | 3 | 7.15 | 78.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.014 | 8.0 |
| 698 | 3 | 7.15 | 80.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.017 | 9.5 |
| 699 | 3 | 7.15 | 82.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.019 | 10.3 |
| 700 | 3 | 7.15 | 84.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.016 | 8.4 |
| 701 | 3 | 7.15 | 89.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.017 | 8.4 |
| 702 | 3 | 7.15 | 97.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.020 | 9.1 |
| 703 | 3 | 7.15 | 101.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.021 | 9.2 |
| 704 | 3 | 7.15 | 114.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 20 | 25 | 0.023 | 8.9 |
| 705 | 3 | 7.15 | 31.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.011 | 15.4 |
| 706 | 3 | 7.15 | 40.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.015 | 16.7 |
| 707 | 3 | 7.15 | 41.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.015 | 15.9 |
| 708 | 3 | 7.15 | 45.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.017 | 16.8 |
| 709 | 3 | 7.15 | 49.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.016 | 14.5 |
| 710 | 3 | 7.15 | 50.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.021 | 18.7 |
| 711 | 3 | 7.15 | 50.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.022 | 19.2 |
| 712 | 3 | 7.15 | 57.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.020 | 15.4 |
| 713 | 3 | 7.15 | 60.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.023 | 17.1 |
| 714 | 3 | 7.15 | 67.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.020 | 13.1 |
| 715 | 3 | 7.15 | 71.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.018 | 11.2 |
| 716 | 3 | 7.15 | 74.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.025 | 15.1 |
| 717 | 3 | 7.15 | 76.8 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.031 | 18.0 |
| 718 | 3 | 7.15 | 78.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.025 | 14.1 |
| 719 | 3 | 7.15 | 80.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.021 | 11.6 |
| 720 | 3 | 7.15 | 80.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.030 | 16.5 |
| 721 | 3 | 7.15 | 87.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.028 | 14.3 |
| 722 | 3 | 7.15 | 92.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.029 | 14.0 |
| 723 | 3 | 7.15 | 103.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.029 | 12.6 |
| 724 | 3 | 7.15 | 127.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 70 | 25 | 0.037 | 13.0 |
| 725 | 3 | 7.15 | 40.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.017 | 18.5 |
| 726 | 3 | 7.15 | 43.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.017 | 17.6 |
| 727 | 3 | 7.15 | 43.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.019 | 19.2 |
| 728 | 3 | 7.15 | 48.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.022 | 20.5 |
| 729 | 3 | 7.15 | 51.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.029 | 25.3 |
| 730 | 3 | 7.15 | 52.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.035 | 30.0 |
| 731 | 3 | 7.15 | 53.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.027 | 22.3 |
| 732 | 3 | 7.15 | 56.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.031 | 24.7 |
| 733 | 3 | 7.15 | 63.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.031 | 21.9 |
| 734 | 3 | 7.15 | 66.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.040 | 26.6 |
| 735 | 3 | 7.15 | 68.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.033 | 21.7 |
| 736 | 3 | 7.15 | 69.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.038 | 24.6 |
| 737 | 3 | 7.15 | 69.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.035 | 22.2 |
| 738 | 3 | 7.15 | 76.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.042 | 24.6 |
| 739 | 3 | 7.15 | 83.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.043 | 23.1 |
| 740 | 3 | 7.15 | 89.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.051 | 25.5 |
| 741 | 3 | 7.15 | 89.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.042 | 20.8 |
| 742 | 3 | 7.15 | 89.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.049 | 24.2 |
| 743 | 3 | 7.15 | 90.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.047 | 23.0 |
| 744 | 3 | 7.15 | 98.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 210 | 25 | 0.048 | 21.8 |
| 745 | 3 | 7.15 | 27.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.026 | 42.8 |
| 746 | 3 | 7.15 | 43.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.039 | 40.4 |
| 747 | 3 | 7.15 | 44.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.032 | 32.4 |
| 748 | 3 | 7.15 | 46.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.035 | 33.9 |
| 749 | 3 | 7.15 | 46.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.034 | 32.9 |
| 750 | 3 | 7.15 | 53.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.044 | 36.3 |
| 751 | 3 | 7.15 | 57.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.053 | 40.8 |
| 752 | 3 | 7.15 | 61.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.053 | 38.1 |
| 753 | 3 | 7.15 | 67.1 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.057 | 37.9 |
| 754 | 3 | 7.15 | 70.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.065 | 41.4 |
| 755 | 3 | 7.15 | 72.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.055 | 34.0 |
| 756 | 3 | 7.15 | 73.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.055 | 33.5 |
| 757 | 3 | 7.15 | 73.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.057 | 34.8 |
| 758 | 3 | 7.15 | 73.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.064 | 38.7 |
| 759 | 3 | 7.15 | 76.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.056 | 32.8 |
| 760 | 3 | 7.15 | 76.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.054 | 31.6 |
| 761 | 3 | 7.15 | 84.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.061 | 32.4 |
| 762 | 3 | 7.15 | 88.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.061 | 30.9 |
| 763 | 3 | 7.15 | 88.9 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.057 | 28.6 |
| 764 | 3 | 7.15 | 91.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 270 | 25 | 0.073 | 35.8 |
| 765 | 3 | 7.15 | 35.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.032 | 40.7 |
| 766 | 3 | 7.15 | 35.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.033 | 42.0 |
| 767 | 3 | 7.15 | 36.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.032 | 39.6 |
| 768 | 3 | 7.15 | 36.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.035 | 43.3 |
| 769 | 3 | 7.15 | 37.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.033 | 39.7 |
| 770 | 3 | 7.15 | 38.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.038 | 44.5 |
| 771 | 3 | 7.15 | 38.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.039 | 45.7 |
| 772 | 3 | 7.15 | 39.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.038 | 43.4 |
| 773 | 3 | 7.15 | 39.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.040 | 45.7 |
| 774 | 3 | 7.15 | 40.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.037 | 41.2 |
| 775 | 3 | 7.15 | 40.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.039 | 43.4 |
| 776 | 3 | 7.15 | 41.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.037 | 40.2 |
| 777 | 3 | 7.15 | 42.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.041 | 43.5 |
| 778 | 3 | 7.15 | 43.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.040 | 41.4 |
| 779 | 3 | 7.15 | 43.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.041 | 42.5 |
| 780 | 3 | 7.15 | 44.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.039 | 39.4 |
| 781 | 3 | 7.15 | 44.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.043 | 43.5 |
| 782 | 3 | 7.15 | 44.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.044 | 44.5 |
| 783 | 3 | 7.15 | 45.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.041 | 40.6 |
| 784 | 3 | 7.15 | 46.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.045 | 43.6 |
| 785 | 3 | 7.15 | 47.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.044 | 41.7 |
| 786 | 3 | 7.15 | 48.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.046 | 42.7 |
| 787 | 3 | 7.15 | 50.0 | 230 | 0.26 | 10 | 1.2 | 0.35 | 0.0017 | 370 | 25 | 0.048 | 42.8 |
| 788 | 3 | 7 | 39.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.046 | 50.7 |
| 789 | 3 | 7 | 43.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.052 | 51.8 |
| 790 | 3 | 7 | 45.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.047 | 45.6 |
| 791 | 3 | 7 | 48.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.067 | 60.8 |
| 792 | 3 | 7 | 48.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.062 | 56.5 |
| 793 | 3 | 7 | 53.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.068 | 56.1 |
| 794 | 3 | 7 | 53.6 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.062 | 51.0 |
| 795 | 3 | 7 | 55.2 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.054 | 43.1 |
| 796 | 3 | 7 | 57.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.074 | 56.5 |
| 797 | 3 | 7 | 59.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.072 | 53.6 |
| 798 | 3 | 7 | 60.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.080 | 58.6 |
| 799 | 3 | 7 | 60.5 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.064 | 46.3 |
| 800 | 3 | 7 | 60.9 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.061 | 44.9 |
| 801 | 3 | 7 | 63.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.078 | 55.0 |
| 802 | 3 | 7 | 63.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.066 | 46.0 |
| 803 | 3 | 7 | 64.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.067 | 46.0 |
| 804 | 3 | 7 | 65.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.077 | 52.1 |
| 805 | 3 | 7 | 67.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.084 | 55.7 |
| 806 | 3 | 7 | 70.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.090 | 56.8 |
| 807 | 3 | 7 | 73.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.076 | 46.3 |
| 808 | 3 | 7 | 75.7 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.085 | 49.6 |
| 809 | 3 | 7 | 76.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.072 | 41.3 |
| 810 | 3 | 7 | 76.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.087 | 50.0 |
| 811 | 3 | 7 | 76.8 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.102 | 58.6 |
| 812 | 3 | 7 | 78.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.082 | 46.0 |
| 813 | 3 | 7 | 79.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.097 | 54.3 |
| 814 | 3 | 7 | 79.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.104 | 58.3 |
| 815 | 3 | 7 | 82.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.080 | 42.7 |
| 816 | 3 | 7 | 85.1 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.101 | 52.1 |
| 817 | 3 | 7 | 95.0 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.107 | 49.2 |
| 818 | 3 | 7 | 95.4 | 230 | 0.26 | 3 | 3.5 | 0.36 | 0.04 | 120 | 25 | 0.096 | 44.5 |
| 819 | 5 | 17.5 | 125.9 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.184 | 26.6 |
| 820 | 5 | 17.5 | 139.4 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.205 | 26.8 |
| 821 | 5 | 17.5 | 178.3 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.263 | 26.8 |
| 822 | 5 | 17.5 | 232.2 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.337 | 26.4 |
| 823 | 5 | 17.5 | 283.1 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.416 | 26.7 |
| 824 | 5 | 17.5 | 335.5 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.485 | 26.3 |
| 825 | 5 | 17.5 | 388.0 | 75.7 | 0.17 | 4 | 3.259 | 0.36 | 0.01 | 150 | 25.6 | 0.549 | 25.8 |
| 826 | 5 | 17.5 | 125.9 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.158 | 22.8 |
| 827 | 5 | 17.5 | 179.8 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.213 | 21.5 |
| 828 | 5 | 17.5 | 230.7 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.265 | 20.9 |
| 829 | 5 | 17.5 | 244.2 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.279 | 20.8 |
| 830 | 5 | 17.5 | 256.2 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.284 | 20.2 |
| 831 | 5 | 17.5 | 283.1 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.315 | 20.3 |
| 832 | 5 | 17.5 | 335.5 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.363 | 19.7 |
| 833 | 5 | 17.5 | 388.0 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.406 | 19.0 |
| 834 | 5 | 17.5 | 440.4 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.459 | 18.9 |
| 835 | 5 | 17.5 | 492.8 | 75.7 | 0.17 | 4 | 2.955 | 0.36 | 0.01 | 150 | 40 | 0.499 | 18.4 |
| 836 | 5 | 17.5 | 179.8 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.184 | 18.6 |
| 837 | 5 | 17.5 | 232.2 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.220 | 17.2 |
| 838 | 5 | 17.5 | 271.2 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.246 | 16.5 |
| 839 | 5 | 17.5 | 284.6 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.256 | 16.3 |
| 840 | 5 | 17.5 | 335.5 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.289 | 15.7 |
| 841 | 5 | 17.5 | 388.0 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.325 | 15.2 |
| 842 | 5 | 17.5 | 440.4 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.358 | 14.8 |
| 843 | 5 | 17.5 | 492.8 | 75.7 | 0.17 | 4 | 2.786 | 0.36 | 0.01 | 150 | 60 | 0.389 | 14.4 |
| 844 | 5 | 17.5 | 127.4 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.138 | 19.8 |
| 845 | 5 | 17.5 | 179.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.160 | 16.2 |
| 846 | 5 | 17.5 | 190.3 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.162 | 15.5 |
| 847 | 5 | 17.5 | 230.7 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.181 | 14.3 |
| 848 | 5 | 17.5 | 283.1 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.201 | 12.9 |
| 849 | 5 | 17.5 | 335.5 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.224 | 12.2 |
| 850 | 5 | 17.5 | 388.0 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.244 | 11.4 |
| 851 | 5 | 17.5 | 440.4 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.265 | 10.9 |
| 852 | 5 | 17.5 | 492.8 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.287 | 10.6 |
| 853 | 5 | 17.5 | 543.7 | 75.7 | 0.17 | 4 | 2.185 | 0.36 | 0.01 | 150 | 80 | 0.306 | 10.2 |
| 854 | 5 | 17.5 | 178.3 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.129 | 13.1 |
| 855 | 5 | 17.5 | 230.7 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.141 | 11.1 |
| 856 | 5 | 17.5 | 269.7 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.148 | 10.0 |
| 857 | 5 | 17.5 | 283.1 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.155 | 10.0 |
| 858 | 5 | 17.5 | 335.5 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.165 | 8.9 |
| 859 | 5 | 17.5 | 388.0 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.177 | 8.3 |
| 860 | 5 | 17.5 | 440.4 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.191 | 7.9 |
| 861 | 5 | 17.5 | 491.3 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.203 | 7.5 |
| 862 | 5 | 17.5 | 543.7 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.215 | 7.2 |
| 863 | 5 | 17.5 | 596.1 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 100 | 0.227 | 6.9 |
| 864 | 5 | 17.5 | 115.4 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.083 | 13.2 |
| 865 | 5 | 17.5 | 127.4 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.088 | 12.6 |
| 866 | 5 | 17.5 | 179.8 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.091 | 9.2 |
| 867 | 5 | 17.5 | 232.2 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.100 | 7.8 |
| 868 | 5 | 17.5 | 284.6 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.105 | 6.7 |
| 869 | 5 | 17.5 | 337.0 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.110 | 5.9 |
| 870 | 5 | 17.5 | 389.5 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.112 | 5.2 |
| 871 | 5 | 17.5 | 441.9 | 75.7 | 0.17 | 4 | 1.731 | 0.36 | 0.01 | 150 | 120 | 0.122 | 5.0 |
| 872 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 3.96 | 0.37 | 0.0333 | 135 | 25 | 0.069 | 39.3 |
| 873 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 3.068 | 0.37 | 0.0333 | 135 | 60 | 0.052 | 29.3 |
| 874 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 2.51 | 0.37 | 0.0333 | 135 | 90 | 0.054 | 30.5 |
| 875 | 8 | 7 | 80.0 | 233 | 0.2 | 7 | 1.59 | 0.37 | 0.0333 | 135 | 120 | 0.021 | 12.2 |
| 876 | 5 | 17.5 | 114.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.070 | 21.7 |
| 877 | 5 | 17.5 | 123.1 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.080 | 20.8 |
| 878 | 5 | 17.5 | 148.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.097 | 21.0 |
| 879 | 5 | 17.5 | 165.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.120 | 20.5 |
| 880 | 5 | 17.5 | 162.2 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.140 | 21.2 |
| 881 | 5 | 17.5 | 179.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.160 | 20.4 |
| 882 | 5 | 17.5 | 184.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.170 | 20.9 |
| 883 | 5 | 17.5 | 193.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.173 | 20.1 |
| 884 | 5 | 17.5 | 198.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.187 | 20.6 |
| 885 | 5 | 17.5 | 198.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.213 | 20.7 |
| 886 | 5 | 17.5 | 215.4 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.263 | 20.4 |
| 887 | 5 | 17.5 | 226.6 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.307 | 20.6 |
| 888 | 5 | 17.5 | 235.0 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.337 | 20.5 |
| 889 | 5 | 17.5 | 251.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.350 | 19.8 |
| 890 | 5 | 17.5 | 237.8 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.367 | 19.7 |
| 891 | 5 | 17.5 | 257.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.370 | 19.2 |
| 892 | 5 | 17.5 | 274.1 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.390 | 19.5 |
| 893 | 5 | 17.5 | 254.5 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.403 | 19.4 |
| 894 | 5 | 17.5 | 262.9 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.417 | 19.4 |
| 895 | 5 | 17.5 | 271.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.427 | 19.1 |
| 896 | 5 | 17.5 | 282.5 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.453 | 18.8 |
| 897 | 5 | 17.5 | 285.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.487 | 18.4 |
| 898 | 5 | 17.5 | 293.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.547 | 17.8 |
| 899 | 5 | 17.5 | 299.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.573 | 17.4 |
| 900 | 5 | 17.5 | 313.3 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.597 | 16.9 |
| 901 | 5 | 17.5 | 321.7 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.620 | 16.5 |
| 902 | 5 | 17.5 | 330.1 | 230 | 0.2 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.637 | 16.0 |
| 903 | 4 | 7.2 | 65.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.045 | 39.5 |
| 904 | 4 | 7.2 | 65.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.052 | 40.5 |
| 905 | 4 | 7.2 | 63.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.059 | 40.2 |
| 906 | 4 | 7.2 | 81.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.072 | 40.7 |
| 907 | 4 | 7.2 | 81.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.078 | 41.3 |
| 908 | 4 | 7.2 | 91.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.084 | 40.3 |
| 909 | 4 | 7.2 | 93.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.094 | 38.9 |
| 910 | 4 | 7.2 | 106.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.101 | 39.4 |
| 911 | 4 | 7.2 | 120.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.107 | 38.8 |
| 912 | 4 | 7.2 | 115.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.113 | 37.8 |
| 913 | 4 | 7.2 | 111.7 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.127 | 38.3 |
| 914 | 4 | 7.2 | 120.0 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.130 | 38.3 |
| 915 | 4 | 7.2 | 128.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.133 | 38.3 |
| 916 | 4 | 7.2 | 158.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.136 | 38.3 |
| 917 | 4 | 7.2 | 128.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.166 | 37.0 |
| 918 | 4 | 7.2 | 158.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.193 | 35.6 |
| 919 | 4 | 7.2 | 188.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.218 | 34.4 |
| 920 | 4 | 7.2 | 218.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.238 | 32.9 |
| 921 | 4 | 7.2 | 248.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.255 | 31.4 |
| 922 | 4 | 7.2 | 278.3 | 90 | 0.17 | 4 | 3 | 0.36 | 0.01 | 150 | 25 | 0.271 | 30.0 |